Mathematical modeling for the crystalization process of hydroxiapatite from whitlockite

Dejeu V.R.a , Barabas R.a, Pop A.a, Bogya E.a, A. Imrea , Agachi P.S. a

aBabes-Bolyai University,Faculty of Chemistry and Chemical Engineering, Department of Chemical Engineering and  Oxide Materials, Arany Janos Str. no. 11, Cluj-Napoca RO-400028, Romania

Abstract

Hydroxyapatites represent a component of the biomaterials, which are largely used in medical applications. In the context of this paper it is studied experimental and theoretic the transformation of beta-whitlokite in hydroxyapatite (HAP). The main factors studied, which influence the process are: temperature, pH and time. A kinetic study was developed regarding the transformation of beta-witlokite in hydroxyapatite at 20-50 °C and pH=8,5-12. The experimental data indicate that, based on the activation energy values  (<25kJ/mol) the rate determining step is the internal diffusion, described by Fick’s law and the mathematical model of the process was stabilized. Interpretation of the experimental data, using the mathematical model, allowed the calculation of the internal diffusion coefficient and its variation with the temperature (obtained values were in the range: 1,8*10-15-5,42*10-15 m2/s ).

Keywords: hydroxyapatite, mathematical model, diffusion coefficient

  - Introduction

Due to the excellent biomedical properties of hydroxyapatite: biocompatibility, bioactivity, boneconductivity, this material was used for medical purposes since 1920 [1,2,3]. The modification produced at the surface of the implant are determined usually by the chemical reactivity, which can be as well influenced by the other properties of the biomaterial as: the size of the particles, composition, porosity, specific surface, structure differences, cristallinity [2].

Literature data [4,5,6] indicate the fact that in the initial step of the precipitation process,  beta–whitlockite (Ca3(PO4)2) with non-crystalline  structure is formed, which,  depending on temperature and pH,  transforms in  hydroxiapatite (Ca5(PO4)3OH).

There are no data about the  rate of transformation of beta-whitlockite in hydroxyapatite. This data are relevant because the crystal size and the morphological structure of hydoxiapatite depends on the value of the rate.

. Z. Bakó & I. Kotsis [6] made a study related to the composition of the calcium phosphate precipitates and the influence of ratio Ca/P, pH and temperature over the conversion of beta-whitlockite in hydroxyapatite. Their conclusion was that the increase of temperature favors the formation of hydroxyapatite due to the intensification of the diffusion processes, without to show how the studied factors influence the diffusion process.

The proposed objective of this paper was the study of the kinetic process regarding the  transformation  of beta-whitlockite in hydroxyapatite and to establish the factors, which influence this process and its mathematical model.

  - Experimental procedure

For the preparation of hydroxyapatite it was described in the paper of Z. Bakó & I. Kotsis [6]. The temperature in the vessel was 200C and 500C and pH=8,7; 9,1; 10,2; 11,3; 12. From time to time samples were taken, the precipitate was filtered, thoroughly washed with bi-distilled water until the NO3- and NH4+ were eliminated and dried at 105 0C for 2 hours. The samples were investigated on a DRON-3 Diffractometer with Cu Kα radiation in the range 15-16 2θ.

  - Results and discussion

The formation of hydroxyapatite by precipitation is a complex process, which includes the following elementary steps:

- the reaction of Ca(NO3)*4H2O and (NH4)2HPO4, resulting beta–whitlockite

- the dissolution of beta–whitlockite

- the formation of hydroxyapatite germs

- the diffusion of the Ca2+ and PO43- ions in the liquid phase and pores

To establish the rate determining step, there were made experimental measurements to study the influence of temperature and pH of precipitation over the formation speed of hidroxyapatite. The evolution in time of the process was traced through the conversion of beta-whitlockite in hydroxyapatite. The influence of pH and temperature over the global rate of the process is plotted in Fig. 1. This figure show that both temperature and pH have a great influence on the formation of the precipitate. At pH=8.5 the conversion of beta-whitlockite in hydroxyapatite reached 49% wt at 20 0C (Fig. 1-b) and 87%wt at 50 0C (Fig. 1-a). For values of pH higher than 8.5, the conversion reaches values of even 100%wt after less than 2-4 hours.

Figure 1. Conversion of beta-whitlockite in HAP at 20 0C (a) and 50 0C (b)

In Fig. 2 is plotted the influence of pH and temperature versus the conversion of beta-whitlockite in HAP at different moments of process evolution. A continuous increase of the conversion versus pH along the development of the process can be observed at 2000÷16000 s with the remark that at 50 0C the influence of the pH is more significant (Fig. 2-b). The =f (time) curve at 20 0C (Fig. 2-a) remains parallel, which indicates the great influence of pH over the conversion. Considering that the transformation of beta-whitlockite in HAP follows a first order kinetics, –ln(1-η)=f (time) was plotted. From the slope of the plot the values of the rate constants listed in Table1 were determined.

X. Zhu [7] sustains that the rate of cristallinity is determined by the value of the activation energy of the atoms, without indicating the values. He affirms that the quantity relation between the rate of the process and temperatures can be expressed by a relation of Arrhenius type: k=k0exp(−EaRT), where k is the rate coefficient, A is a constant, Ea is the activation energy, R is the universal gas constant, and T is the temperature (in degrees Kelvin).

Starting from this hypothesis, the dependence –ln k=f (1/T) was plotted; from the slope of the curve the energy of activation was calculated; the values are shown in Table 1. It was found that the activation energy has in all cases values in the range: 3,43-4,75 kcal/mol, which indicates that the limiting process is the diffusion.

Figure 2. The influence of pH and temperature over the global rate of the process at 20 0C (a) and at 50 0C (b)

Table 1. The values of the rate constants and the activation energy

| pH | ln k1 20 0C | ln k2 50 0C | Ea [kcal/mol] |
| --- | --- | --- | --- |
| 9,1 | -9,33 | -8,78 | 3,43 |
| 9,7 | -9,21 | -8,51 | 4,37 |
| 10,2 | -9,18 | -8,47 | 4,43 |
| 11,3 | -9,15 | -8,42 | 4,56 |
| 12 | -9,13 | -8,37 | 4,75 |

Intense mixing of the stirrer (intense hydrodynamic conditions from liquid phase) and the small dimensions of the channels from the inside of the crystals suggested us that limitative step is the internal diffusion through the pores.

The kinetic equation, which stays at the base of the mathematical description of the trasformation process of beta-whitlockite in hydroxiapatite is given by the Fick’s law:

dnHAPSdτ=−D0dCHAPdr	(1)

where D is the diffusion coefficient,  CHAP is the concentration, nHAP is the number of mols and surface S=4r2, where r is the radius of the hydroxiapatite crystal at one moment .

The integration of the equation (1) gives:

−dnHAPdτ1r−1R=4πD0CHAP	(2)

where dnHAP=ρ⋅4π r2⋅dr, ρ=ρ⋅V⋅XM (where is the density, X is the weight ratio, M is the molecular weight, V is the volume of the hydroxiapatite particle.  The relation between the transformation rate, the radius at one moment r and final radius R is given by the relation: η=R3−r3R3, which leads to:

11−η13−1dηdτ=3D0ρ⋅R2CHAP	(3)

Taking into consideration that the solubility of HAP (CHAP) is constant the integration of equation (3) gives:

τ=16ρR2D0CHAP[1−3(1−η)23+2(1−η)]	   (4)

Table 2. The values of the diffusion coefficient

| pH | D01 [m2/s] ·1015 20 0C | D02 [m2/s] ·1015 50 0C |
| --- | --- | --- |
| 8,5 | 1,90 | 5,42 |
| 9,1 | 1,87 | 5,36 |
| 9,7 | 1,85 | 5,23 |
| 10,3 | 1,84 | 5,21 |
| 11 | 1,81 | 5,16 |
| 12 | 1,80 | 5,12 |

Fitting the experimental data by the integration method -F(where F( allows the deduction of the diffusion coefficients from the slope tgα=1τρR2D0CHAP (Table 2). Their analysis shows that the diffusion coefficients are influenced by temperature and the values obtained fit to the literature data (10-12-10-15 m2/s)  [8,9].

  - Conclusions

- The influence of the temperature and pH on the transformation rate of the beta-whitlockite in hydroxyapatite was investigated

- From experimental data the k constant and the activation energy of the process were calculated

- The obtained small values of the activation energy (Ea<6 kcal/mol) shows that the rate determining step is the diffusion.

- The mathematical model of the transformation of beta –whitlockite in hydroxyapatite and the diffusion coefficients was established

The determination of the numerical values for the diffusion coefficient D0 will allow, using the proposed model, to solve the simulation and optimization problems of the process.

References

1. Xiaolong Zhu, Nano Hydroxiapatite/Collagen, Nano Hydroxiapatite and Anodic Oxides on Titamun, 2005

2. Z. Bako, I. Kotsis, Composition of precipitated Calcium Phosphate Ceramics, Ceramics International, 18, 1992, 373-378

3. M. Vallet-Regi, Ceramics for Medical Applications, J. Chem. Soc., Dalton Trans.,2001, 97-108

4. S. Zhang, K. E. Gonsalves, Preparation and Characterization of Thermaly Stable Nanohydroxiapatite, Journal of Materials Sciece: Materials in Medicine, 8, 1997, 25-28

5. E. C. Moreno, T. M. Gregory, W. E. Brown, Preparation and Solubility of Hydroxiapatite, Journal Research of the National Bureau of Standards-A. Phsysics and Chemistry, 72A, 6, November-December 1968

6. L. C. Chow, L. Sun, B. Hockey, Properties of Nanostructural Hydroxiapatite Prepared by a Spray Drying Technique, 109, 6, November-December 2004

7. C. S. Chai, B. Ben-Nissan, Bioactive Nanocrystaline sol-gel Hydroxiapatite Coatings, Journal of Materials Science: Materials in Medicine, 10, 1999, 465-469

8. K. M. Allal, M. Abbessi, A. Mansour, a., Trans. Chem. E., 70, part. B, 1992, p.140

9. G. Mura, A. Lallai, P. Olla, Chem. Eng. J., 1, 1991